### Product Name

## LexCore™

## Manufacturer

CSS-Specialty Products

PO Box 29

Kirkwood, NY  13795

Phone 607-238-0317

Fax Line 607-238-0981

Watts Line 888-673-8540

E-mail: info@cssystems.us

###### Product Description

LexCore panels consist of fire resistant gypsum board and LEXAN®.

They are available with 5/8” or  3/4” cores  and in four increasingly higher levels of impact resistance:

LexCore LC-5810

(5/8” FIRECODE C w/.010” LEXAN)

LexCore LC-5820

(5/8” FIRECODE C w/.020” LEXAN)

LexCore LC-5830

((5/8” FIRECODE C w/.030” LEXAN)

LexCore LC-5881

(5/8” FIRECODE C w/.081” LEXAN)

LexCore LC-3410

(3/4”  ULTRCODE w/.010” LEXAN)

LexCore LC-3420

(3/4”  ULTRCODE w/.020” LEXAN)

LexCore LC-3430

(3/4”  ULTRCODE w/.030” LEXAN)

LexCore LC-3481

(3/4”  ULTRCODE w/.081” LEXAN)

## Basic Use

LexCore is utilized for security walls and barriers in prisons, jails, hospitals, schools, and municipal buildings.  It is typically used in holding cells, interrogation rooms, housing areas, hallways and high traffic corridors adjacent to secure areas.

### Standard Dimensions

LexCore is supplied in 4’x 8’ panels.  Lengths of 9’ and 10’ are available on

special order.

UL – Fire Rating:

One hour when using 5/8” FIRECODE C core gypsum panels and two hours when using 3/4” ULTRACODE core gypsum panels.

LexCore 5/8” & 3/4” panel systems meet the following UL Designs.

U-495, V-409, V-410, V-412, V-416 and Canadian 495.

Installation

##### Installation of LexCore wallboard should be consistent with methods described in the Gypsum Association GA-216 (Application & Finishing of Gypsum Board).

The LEXAN side is always installed facing the studs and is not the exposed surface.

Advantages

The composite configuration simplifies installation.

The LEXAN substrate is virtually impenetrable allowing surface damage to be readily repaired in place.

###### Guide Specifications

Part 1.  General

Work under this section is subject to the provisions of the contract and the contract documents that affect the work specified herein.

1.1 Scope

Furnish and install LexCore, fasteners, joint compounds, and tapes as specified to meet project requirements.

1.2 Delivery / storage of materials

All materials shall be delivered in their original unopened packages and stored in an enclosed shelter providing protection from damage and exposure to the elements.

1.3 Handling

Handle material in the same manner as gypsum to protect edges and corners. Do not slide drag or drop LexCore panels.

1.4 Quality Assurance

Submit LexCore samples and manufacture's literature as required by owner.

Part 2. Product

2.1 Materials

Two ply laminated composite panels comprised of gypsum, polycarbonate and adhesive.

Part 3. Execution

3.1 Fabrication

Standard power tools equipped carbide blades and bits are adequate for cutting and routing LexCore panels.

The LEXAN layer should be cut completely through, then the gypsum board layer may be scored and snapped.

3.2 Installation

LexCore is installed and finished using the same techniques as required for standard gypsum board.

Corrosion resistant, drill point, bugle head screws (1 1/4” minimum length) are recommended to secure the panels with the LEXAN surface facing the studs.

3.2 Finishing

Finishing procedures, such as taping and spackling are the same as for standard gypsum board.

# Text boxes

LexCore LC

Standard Series

LexCore panels provide high-impact, penetration-resistant wall strength for security walls and barriers in prisons, jails, hospitals, schools and municipal buildings.

Specific applications include holding cells, interrogation rooms, housing areas, hallways and corridors, and office areas located adjacent to secure areas.

When in place, LexCore panels are finished using the same techniques as those required for standard gypsum wallboard installations.

09250

09250

LEXAN is a registered trademark of General Electric Co.

FIRECODE  is a registered trademark of USG Corporation

ULTRACODE  is a registered trademark of USG Corporation

LexCore is a trademark of Contemporary Storage Systems

LC 06-13-03