POWDER CRAFT INC.

ESTABLISHED 1989

 SERVICES 

  Custom Powder Coating

  Abrasive Blast Stripping

  Plastic Media Blasting for small parts

  Burn Off Oven Stripping

FACILITY-EQUIPMENT

  12,000 Square Feet Shop Area

  14' x 34' Indoor Blast Room

  3/4 Ton Monorail Material Handling

  Dock and Drive In Truck Loading

 FEATURES 

  Large Items (1 ton & 24' length)

- 25'L x 14'H x 10'W Curing Oven

(largest batch oven on East coast)

  Turnaround usually 10 Working Days

  Flexible Scheduling

  NO Minimum Lot Sizes

  Large Color Selection

  Customer Materials Fully Insured

(at our plant and for return shipping)

  Workmanship guaranteed for 1 year

POWDER COATING

 WHAT IS IT ?? 

  Epoxy, Polyester, Urethane formulations

- A dry coating is applied with an electro-static spray and cured at 375-400 F

  "Dead" flat to high gloss level finishes

- Smooth, textured and wrinkle, clear, fluorescent, specialty colors

 APPLICATIONS 

  Industrial and electrical enclosures

  Wrought iron and aluminum railing

  Auto frames and race car chassis

  Vehicle wheels and suspension parts

  Major appliances - outdoor furniture

  Fabricated structures and machinery

  Protection for any metallic surface

 WHAT'S DIFFERENT ?? 

  Environmentally friendly - NO solvents

  Nonporous surface / excellent adhesion

  Flexible yet abrasion and chip resistant

  Outstanding chemical resistance

  NO runs or sags even with tube construction

  Adheres to non-ferrous metals

POWDER CRAFT, INC.

610-280-3770/fax 610-280-3763

#### Contract and Custom Powder Coating Services

##### Serving OEM, Commercial and Retail customers since 1989

25 Foot Batch Oven

300 + Stock Colors

No Minimum Lot Size

Flexible Scheduling

Quick Turnaround

Large or Small Parts

Work Guaranteed / Insured

### HOURS: M-F 8:00 to 5:30

Powder Craft, Inc.

###### 4 Tabas Lane, Exton, PA  19341-2753

610-280-3770 / fax: 610-280-3763

E-mail:  info @ powdercraft.com

or visit:  www.powdercraft.com

Member of the Philadelphia Better Business Bureau and the Powder Coating Institute

 What we do for you 

Unless there are special circumstances or instructions, your parts will be given a light abrasive treatment (grit blast) to rid the surface of any oxidation formed since it was stripped and to provide a slight etching of the surface for improved coating adhesion.  The parts are then treated with a corrosion protective solution (steel and aluminum receive different treatments).  Masking is done where required and the parts are coated.

Our workmanship is guaranteed for 1 year under normal service!  If you have any other questions, give us a call!

 Surface Preparation 

CLEANING / DEGREASING:  All parts to be coated must be free of dirt and oils; parts should be cleaned and degreased prior to shipment.  This is a very important step prior to any type of coating and especially so for powder coating since the curing temperatures will drive oils, grime, and moisture out of the part and cause pitting and other damage to the paint as it cures.  For best results, take it apart if it will come apart to ensure that there are no hidden contaminants to mar the finish.

STRIPPING:  Parts must be free of all coatings prior to powder coating.  Powder Craft can have chemical stripping done at a local facility and bill separately (as a service to you) or we can sand blast (using an 80 grit aluminum oxide) at our facility.  However, this is an area where you may be able to save on out-of-pocket expense and minimize the turn-around time in our shop if you choose to do your own stripping.  Since there are so many variables when stripping parts, we will not quote prices.  However. if you call, we can tell you what work similar to yours has been costing.  We use Redi-Strip of Allentown, PA for chemical stripping.  Parts come back totally rust free and require a minimal amount of prep prior to coating.

MASKING:  Unfortunately, you cannot mask surfaces before sending parts to us.  It would make our job a lot easier but the pretreatment and chemicals used by Powder Craft to prepare parts prior to coating would damage any masking you would do.  However, it is very important that you clearly indicate any areas you wish masked so we can do a proper job after completing our preparation steps.  (Please use tape or write any special instructions – DO NOT write on or mark the parts.)  Powder coatings have a greater ability to get into corners, holes, and threaded areas than liquid spray paints and while the coating is relatively thin, it could cause some interference during assembly.  It is possible that masking is not required; it may be simpler (for us) and less expensive (for you) if you choose not to mask but to chase the threaded holes with a tap and run a drill through bored holes after the parts are returned.

 Suggestions 

Once parts are stripped and cleaned the surface should be prepared.  For an optimum finish; debur edges, remove all weld spatter, and grind and sand all rough spots.  The smoother the surface, the better the finished product.  But don't polish the surfaces, unless you are having a special coating applied, since parts will normally get blasted (see above).  Note that powder coatings are relatively thin and will not fill rough surface texture caused by rust pitting, gouges, excess weld/braze material or spatter, and casting marks.  While "bondo" will melt in the oven, you can use body solder, silver solder, or braze to fill and then grind smooth.  We have also found a "use out of the can" product which will withstand the heat.

 Inventory 

PLEASE!!!!   Provide us with an inventory of  your parts when shipping items so can be sure that nothing is thrown away with the packaging.

Powder Coating Costs Less

Powder coating prices are typically less than those of liquid coatings when one considers the cost of quality primers and the color coat alone.  The increased durability provided by powder coatings is a further plus.

Our pricing is based on time and material.  The following are average prices for our standard process of blast cleaning, anti-corrosion coating, masking, coating with black or white powder, and packing.  Your price may vary depending on quantity of parts and/or linear feet, size and weight, condition, color desired, and other services you wish us to provide.

RAILING  --  $4 to $32 per linear foot depending on type of construction, material and quantity.

FRAMES

Auto – street legal	$460 - 650

Dragster	$450 - 625

Karts	$140 - 250

MicroSprint/Sprint	$275 - 425

Cycle	$250 - 325

1/4 Midget	$175 - 210

Ultralight	$375

LAWN FURNITURE	$70 per seat

WHEELS

Alloy	$85

Alloy-Cycle	$105

Steel	$55

BOAT radar arch	$410

SPIRAL staircase-1 story	$520

- A more complete automotive price list is available

- Quotes provided upon request