WHY 12 STRANDS?    WHY CANAM?

COMPLIES WITH U.S. Forest Services   RFP # 49-02-07

High Strength:	        7:1 Safety Factor

Max. Elongation:    5% Stretch  						PLASMA 12 Strand

TESTED:	        2 ½ times safe working load, CERTIFIED			             	        ELIMINATES 5% Stretch 	during operation	             Plasma 12 strand

CUSTOM MADE:  Rope Length / Cover / Thimbles

Plasma 12 Strand is the highest strength synthetic rope available

All Long Lines are:	PRE-STRETCHED prior to shipping.

SPLICED using Standard Galvanized Thimbles or Blue Line Tubular Thimbles

ID TAGGED, and Owner/Operator Historical Record is provided

Options Available:	THIMBLE:  		Galvanized Steel Thimble or Blue Line Tubular Thimble

COVERS:     		Orange Velcro, Polyester  with Return Ends.

2”-3” Clear Vinyl Tube Hose.   (customer request)

ELECTRICAL:	 3Wire; HiWire or 14/3 Gauge

Standard Connector or custom (customer request)

| PLASMA | size circ weight | Safe work | load | Min. Tensile Strength |
| --- | --- | --- | --- | --- |
| ROPE SIZE | mm inch lbs./100ft kg/100m | LBS. | KG | LBS | KG |
| 7/16" | 11 1 1/4" 4.2 6.3 | 3000 | 1350 | 21,000 | 9,500 |
| 1/2" | 12 1 1/2" 6.4 9.5 | 4400 | 2000 | 31,300 | 14,200 |
| 9/16" | 14 1 3/4" 7.9 11.8 | 5400 | 2500 | 37,900 | 17,200 |
| 5/8" | 16 2 10.6 15.8 | 7300 | 3300 | 51,400 | 23,300 |
| 3/4" | 18 2 1/4" 13.3 19.8 | 9700 | 4500 | 68,500 | 31,100 |
| 7/8" | 22 2 3/4" 19.6 28.8 | 13200 | 6000 | 92,500 | 42,000 |
| 1 " | 24 3 23.4 34.9 | 15700 | 7100 | 110,000 | 49,900 |
| 11/8" | 28 3 1/2" 31.9 47.6 | 21000 | 9500 | 147,000 | 66,700 |
| 1 1/4" | 30 3 3/4" 36.2 54 | 23500 | 10600 | 165,000 | 74,800 |
| 1 5/16" | 32 4" 41.7 62 | 28000 | 12700 | 196,000 | 88,900 |
| 1 1/2" | 36 4 1/2" 51.7 77.1 | 31500 | 14280 | 221,00 | 100,000 |

Plasma 12     Strand  with  Swivel and   Hook & Cage

Note:

Universal Joint

is connecting              the Swivel to     the Hook

Blue Line Thimble                                                       Orange Cordura Jacket with Velcro